## Slide 1
Influences of Doping, Porosity, and Anisotropy on the Critical Currents of Magnesium Diboride Wires
M.A. Susner
M.D. Sumption
G.Z. Li
Y. Yang
and E.W. Collings
M.A. Rindfleisch
M.J. Tomsic

## Slide 2: Acknowledgements
This work was funded by the Unites States Department of Energy, Office of High Energy Physics and the State of Ohio
A portion of the data in this work was collected at the National High Magnetic Field Laboratory at Florida State University

## Slide 3: Summary of Unanswered Questions in MgB2
How do we separate intrinsic properties like J0, Bc2 and γ from extrinsic effects like porosity and the presence of blocking phases ?
What are the influences of Bc2, γ, porosity, and connectivity on Jc, Fp(B)?
Have compared microstructure and superconductive properties of three different systems to isolate these effects
PIT (porous, randomly oriented)
IMD (dense, randomly oriented)
Films (dense, aligned)

## Slide 4
BF TEM MgB2 wire x-section
MgB2 wires consist of randomly oriented, polycrystalline grains ~50-100 nm in size, largely dependent on prior B size
FIBed MgB2 wire x-section

## Slide 5: TEM- PIT wires
Mg readily passivates- forms MgO and Mg(OH)2
Drawing deforms the Mg, creating fresh surfaces
HT (where the prior Mg, through vapor diffusion, infiltrates the B to form MgB2) leaves behind MgO
See MgO surrounding every prior Mg stringer
If we assume this cross section is representative of the entirety of the sample, then we see only 47% of the sample is free of porosity, MgO, or other second phases

## Slide 6: TEM- PIT wires
These MgO precipitates and the high degree of porosity serve to inhibit connectivity (i.e. supercurrent flow) in MgB2 wires
Summary:
PIT wires both
-randomly oriented
-porous and poorly-connected

## Slide 7: PLD synthesized thin films
MgB2
SiC
Pt
200 nm
PLD-synthesized MgB2 thin films result in c-axis oriented thin films
Randomly oriented in-plane, columnar grains
Summary:
MgB2 thin films both
-c-axis aligned
-well-connected
500 nm
Pt cap layer from FIBing
MgB2
SiC

## Slide 8: Comparison of superconductive properties?
Normalize to B(Fp,max)
Polycrystalline randomly oriented grains in wires yield significant deviations at high b when combined with high porosity
Thin films and dense wires deviate less
Therefore, it is reasonable to assume that Porosity and connectivity are as large of an influence as the intrinsic anisotropy
Let’s quantify this…

## Slide 9: Quantifying effects of porosity and anisotropy
For a superconductor, α =  & t = 1.76
Deutscher et al. J. Phys., Lett. vol. 40, no. 10, pp. 219–21, 1979.
p is probability that a component of the network is conducting
pc is percolation threshold (minimum fraction of conducting regions for cont. current path)
p is probability that a grain is superconducting
pc is percolation threshold
ps is phase fraction (excluding pores, secondary phases, &c.)
Here we use Eisterer’s analysis for percolative current paths in MgB2
M. Eisterer, M. Zehetmayer, and H. W. Weber (2003) Phys. Rev. Lett., 90(24) 247002 and M. Eisterer et al. (2009) SuST 22(3) 034016.
Straley and Kenkel modeled a network of non-linear I-V resistors following the power law
See Phys Rev. Lett. 49(11) 767-770 (1982) and Phys. Rev. B 29(11) 6299-6305 (1984)

## Slide 10: Applying the model for MgB2
For an anisotropic superconducting material…
For a grain-boundary pinned superconducting material…
Create a network of 104 grains, each with (sin q) randomly distributed between 0 and 1
0o: “out-of-plane” Bc2- lower value
90o: “in-plane” Bc2- higher value
Here we use Eisterer’s analysis for percolative current paths in MgB2
What are the effects of each of these variables?

## Slide 11: Anisotropy
Increase g
Use a model undoped MgB2 system:
-J0: 5x106 A/cm2
-Bc2: 20 T
-pc: 0.2- densely packed system
Increasing γ causes a decrease in the amount of supercurrent percolation paths
As a result, Jc at high B decreases – this effect intensifies with increase in γ

## Slide 12: Percolation Threshold
Increase pc
Anisotropy (γ) fixed to 2.5
This value is lower than that seen in single crystals or thin films but typical for what is seen in wires (B purity, grain size, defects)
Increasing pc a more subtle effect than anisotropy- effect small at low B, large at high B

## Slide 13: Porosity
decrease ps
Increase porosity
Anisotropy (γ) fixed to 2.5
pc: 0.2
Bc2: 20T
J0: 5x106 A/cm2
Porosity globally decreases Jc(B)

## Slide 14: Fitting Percolation Model to Real Wires
Need to fit 5 parameters:
γ, pc, ps, Bc2, J0
Can obtain experimental values for γ, Bc2, J0
Can make the assumption that ps=0 (or close to it) for IMD samples, leaving just one parameter necessary for fitting: pc

## Slide 15: Finding Bc2

## Slide 16: Finding Bc2
Bc2,0K ~ 30 T

## Slide 17: Anisotropy
Isolating γ for a nano-polycrystalline material is problematic
Can estimate based on:
M. Eisterer, M. Zehetmayer, and H. W. Weber (2003) Phys. Rev. Lett.
When we assume 0.2<pc<0.3
(reasonable estimate typical to literature)
we get 2.1<γ<3.1
Now we have reasonable starting values for J0, γ, and Bc2

## Slide 18: IMD, 2% C-doped
Used experimentally determined g, J0, Bc2 for initial fitting parameters
IMD wire was assumed to be 100% connected (i.e. no porosity) in fitting
Assumption valid in comparison to PIT wires

## Slide 19: PIT ~2% C-doped
Assumed properties within a fiber are the same as IMD  porosity/MgO layers only difference

## Slide 20: Summary and Implications
 | MgB2-IMD | MgB2-PIT
J0 | 1.1 x 107 A/cm2 | 1.1 x 107 A/cm2
Bc2 | 32 T | 33 T
γ | 2.6 | 2.6
pc | 0.2 | 0.2
ps | 1 | 0.67
p*= pc/ps | 0.2 | 0.30
Acon= [(ps-pc)/(1-pc)]1.76 | 1 | 0.59
At 4.2 K, 10 T, the decrease in Jc seen in MgB2 compared to a theoretical, dense, isotropic material is
~60% due to anisotropy
~40% due to porosity
Anisotropy limits high field Jc (not new)
Decreasing porosity can mitigate this effect
Additionally, anisotropy can be further reduced with increased doping
See M.A. Susner et al. (2011) SuST 24 012001/1-5

## Slide 21: Next Step
Based on this understanding, and feedback with our collaborators at Hypertech…
Following the RLI process of Giunchi… one achieves good material density
Following Kumakura’s IMD results… one achieves good Jc
We get good Jc with SMI pre-doped nano-B as a result of increases in Bc2, decreasing porosity, and decreasing γ

## Slide 22: Conclusions
Much research in MgB2 focused on improving Bc2, Fp, Jc, &c.
A complete deconvolution of connectivity, pinning, anisotropy, Bc2, and porosity was possible using PIT, IMD, and thin film MgB2 samples
Previous work has led to the conclusion that MgB2 is not ideal for high field applications due to its anisotropy
Careful synthesis of wires with reduced anisotropy and porosity can increase high field properties (e.g. 10 T) by an order of magnitude
Application of percolation theory to MgB2 wires of different designs isolated the effects of porosity and crystalline anisotropy. Unappreciated to date, porosity was seen to be just as important a factor as g
  In particular, at 10 T, 60% of supercurrent degradation comes from anisotropy, 40% from porosity
  Can nearly eliminate the latter, reduce the former through doping

## Slide 23: Questions?
Thank you!