## Slide 1: Prospects of Nb3Sn performance enhancement for high field fcc applications
Mike Sumption, X. Xu, and E.W. Collings
Center for Superconducting and Magnetic Materials, MSE, The Ohio State University
This work was supported by the U.S. Department of Energy, Office of Science, Division of High Energy Physics, under SBIR phase I DE-SC0013849 and University Grant DE-SC0011721.
Hyper Tech Research, Inc.
Xuan Peng
Mike Tomsic
Selected data from
SupraMagnetics, Inc.
Leszek Motowidlo

## Slide 2: Nb3Sn based Conductor Options
Bruker PIT Conductor
At 15 T Jc is 2700 A/mm2, JnonCu (RRP) = 1600 A/mm2, and Tube/PIT 1350 A/mm2

## Slide 3: Need of FCC for improved Nb3Sn
Needed conductor amount for FCC
FCC with 16 T magnets: 4,500 tons of Nb3Sn and 10,000 tons on NbTi
FCC with 20 T: 1,400 tons HTS, 6,300 tons Nb3Sn, 11,000 tons NbTi
Conductor Specifications?
  Non Cu Jc of 1500 A/mm2 at 16 T?
Will need both ternary alloy and enhanced pinning

## Slide 4: Possibilities for Nb3Sn Jc enhancement
Keep pinning the same but enhance Jc further from the presently optimized ternary (In principle maybe possible, but so far difficult)
Enhance pinning in Binary
Enhanced pinning in similar-to-present ternary alloy

## Slide 5: Importance of refining Nb3Sn grain size
Experiments (Dietderich, 1997) on films (electron-beam co-evaporation deposition): as grain size is very fine, the Fp-B curve peak shifts to 0.5Bc2.
How to obtain such small grain size in practical strands?
Reducing reaction temperature? Cannot go to < 80 nm.
Adding second phase particles to prevent grain coarsening?
For present strands, reducing grain size leads to increase in Fp,max, but Fp,max is always at 0.2Bc2.
15-30 nm
50-100 nm
The high-field Jc can be significantly improved by shifting Fp,max to 0.5Bc2.
D. R. Dietderich and A. Godeke, Cryogenics 48, 331 (2008).
Maximum pinning force Fp,max
Bc2
0.2Bc2

## Slide 6: Refine Nb3Sn grain size by adding second phase particles
“Internal oxidation”: O diffuses in an A-B solid solution, and selectively oxidizes the solute B, forming BOn particles in matrix A.
Prerequisites:
B is much less noble than A.
O diffuses fast in matrix A.
O partial pressure is only high enough to oxidize B.
Methods | Effect | Problems
Add Y or Gd into Nb melt: form Y or Gd particles. | At 750 C, 0.75 % Y refines grain size from 400-500 nm to 200-300 nm. | Y or Gd particles harden Nb alloy, making processing impossible.
The particles can only be formed during heat treatment.
Billet of Sn, Cu, Nb alloy
Final-size strand
Superconducting Nb3Sn
Extrusion, drawing
Heat treatment
Procedures to fabricate Nb3Sn:
One method: internal oxidation.
A-B alloy
O source
JO
CO
CB
BOn
Zone I
Zone II
C
For the case of Nb3Sn, we can use Nb-Zr alloy, since Zr is much less noble than Nb.

## Slide 7: Can the internal oxidation method work for Nb3Sn wires?
Cu stabilizer
Nb-1 at.%Zr
Cu
Sn core
Inter-granular ZrO2 particles
Intra-granular ZrO2 particles
During heat treatment:
Pure Ar atmosphere: no oxygen supply
Ar-O mixture: sufficient O supply
First, etch off the outside Cu to expose Nb-1Zr to the atmosphere.
How do ZrO2 particles refine Nb3Sn grain size?
Impede Grains coarsening: distinct gradients in grain size.
Be nucleation centers: newly-formed grains in the internal oxidation samples are smaller.
X. Xu et al., Appl. Phys. lett. 104, 082602 (2014)
Reacted in pure Ar
Reacted in Ar-O
750 °C
Earlier-formed Nb3Sn grains
Newly-formed Nb3Sn grains
Nb
To find out if this internal oxidation method really works for Nb3Sn strands, we made an experimental monofilament:
Note ZrO2 particles 10 nm OD

## Slide 8: Supplying oxygen to Nb-Zr alloy in real strands
The diffusion of O in Cu layer: assuming CO(O) = Cs, CO(Nb) = 0.
T, 600 °C | O in Cu
D, μm2/s | 100
Xs, at.% | 10-5
Oxide and Nb-Zr do not have to contact. As long as the atmosphere is connected, O can be transferred via atmosphere.
1. Supply O externally during heat treatment?
Little O is absorbed by Nb-Zr.
O2
O2
O2
O2
Oxide powders that can supply O to Nb:
CuO, SnO2, ZnO, Nb2O5.
Oxide powders that cannot supply O to Nb:
NbO or NbO2.
In this work we will use oxide powder as O source, because powder possesses good flowability during wire processing.
The goal is to transfer the O from oxide powder to Nb1Zr during heat treatment.
Cu
Nb
ri
ro
O2
O2
O2
O2

## Slide 9: An example tube type monofilament
Cu
Nb-1Zr
SnO2
Cu
Sn core
A green-state subelement:
SnO2
200 nm
200 nm
NbO2
SnO2 powder: 625 °C:
Wires with NbO2 and SnO2: 650 C for 150 h:
NbO2: < 0.3at.% O, SnO2: supplied >3 at.% O.
Average grain sizes: 104 nm and 43 nm.
SnO2-650 °C / 400h:
A control: NbO2, which does not supply O.
The 12 T layer Jc of the state-of-the-art Nb3Sn strands is 5 kA/mm2, so the SnO2-625x800h doubles this record.
Ave: 36 nm
Hyper Tech- Ohio State application

## Slide 10
Fp-B curves of Internal oxidation strands
As grain size d is < 50 nm, reducing d shifts the curve both to the up and to the right.
Fp,max vs reciprocal of grain size:
Normalized Fp-B curves:
Bc2 was obtained by fitting the Fp-B curve using Fp=Kbp(1-b)q.
Two companies are using this technique to fabricate products.
With the same Nb3Sn phase fraction
0.25 mm

## Slide 11
Parameters | Present best | Internally oxidized
Bc2 (4.2 K), T | 25 T | 25 T
Grain size, nm | 100 – 150 | 25 nm
Fp-B peak | 0.2 Bc2 | 0.5Bc2
Fp,max, GN/m3 | ~90 GN/m3 | ~250 GN/m3
Suppose we can further refine grain size, what will be the Jc?
4
6
1
State-of-the-art RRP wires with 4.2 K, 12 T non-Cu Jc of 3000A/mm2.
Suppose grain size is refined to 20-25 nm with Bc2 kept at 25 T.
A Nb-2%Zr sample reacted at 650 °C:
Average grain size: 34 nm.
Using Nb-2%Zr, 25 nm of grain size is likely reachable.
With grain size of 25 nm and Bc2 = 25 T, what’s the Jc?
Nb-1Zr + SnO2 at: | Bc2, T | Grain size | Fp-B curve peak | 12 T layer Jc, A/mm2
650 C | 23 | 45 nm | 0.26Bc2 | 8500
625 C | 20 | 36 nm | 0.34Bc2 | 9600

## Slide 12: Observations and Plans
Factors we can control: chemistry/processing
Composition/Microstructure
Bc2
Properties
Performance
Fp,max
Peak field
Nb3Sn phase fraction
High-field Jc
Additions: Ta/Ti
Sn content
Grain size
1. Starting Nb/Sn/Cu ratio
2. Precursor architecture
3. Doping: Nb-Ta, Sn-Ti
4. Heat treatment: temperature, time
5. Other approaches: e.g., internal oxidation
Observations:
Ic of Nb3Sn strands can be improved by improving: Nb3Sn fraction, Bc2, and Fp,max.
There is still some room for Bc2 improvement by enhancing Sn at.%. A model has been developed on what determines Sn content of Nb3Sn and how to control it.
There is huge room for Jc improvement via grain size refinement. An internal oxidation method is proposed, and has been proven very effective.

## Slide 13
Some Questions we might ask
Q1: what Nb3Sn strands can this method be used in?
Q2: is it feasible to make practical strands?
Q3: Does the high Jc only exist in a very thin layer?
Q4: Is the refined grain size at the expense of Birr?
Q5: Can we shift the Fp-B curve peak to 0.5Birr?
Q6: Does this Hinder Margin?
Q7: Can we realize this for a multifilamentary ternary?

## Slide 14
Q1: what Nb3Sn strands can use this method?
PIT:
Not Only Tube Conductor, but PIT, Bronze, or Internal Sn distributed barrier (e.g., RRP) –
As long as a structure allows for the addition of oxide powder in a proper position, so that oxygen can be transferred, this structure is OK.
Patent: Xu, Peng, Sumption, PCT/US2015/016431.

## Slide 15
Q2: the feasibility of making practical strands
Supramagnetics’ PIT (120-sub): dsub ≈ 50 μm
As to the application of this method, the biggest concern lies in the drawability of Nb-Zr alloy. But this appears not be a problem for strands up to 120 stack
We reported high Jc on a monofilament, but if this technique can not be used to make practical wires, then it is useless.
Hyper Tech’s PIT (61-sub): dsub ≈ 38 μm
Demonstration of making practical Tube and PIT strands:
0.4 mm
0.82 mm

## Slide 16
Q3: Does the high Jc only exist in a very thin layer?
8 μm
650 C x 400h
Fine grain size and associated high Jc can exist in a very thick Nb3Sn layer:

## Slide 17
Q4: Is the refined grain size at the expense of Birr?
Conclusion: introducing ZrO2 particles and refining grain size do not decrease Birr of Nb3Sn strands relative to those ordinary strands. But we do need: 1, full reaction; 2, Ta or Ti addition.
With proper addition, we can push the Birr to 25-26 T.
Fischer, Lee, Larbalestier, PIT, 675 °C:
4.2 K
Need ternary addition: Ta or Ti.
Does refined grain size => reduced Bc2?
An ongoing experiment: Ti doping

## Slide 18
Q5: Can we shift the Fp-B curve peak to 0.5Birr?
36 nm grain size => Fp-B curve peaks at 1/3Birr. Mechanism?
Point pinning by ZrO2 particles: Fp = C∙(B/Birr)∙(1-B/Birr)2? If so, Fp-B curve peak can only shift to 1/3 of Birr.
Refined grain size matching flux line spacing? If so, Fp-B curve peak can shift to 1/2 of Birr.
Which is correct?
(~45 nm)
(~90 nm)
(~36 nm)
An extrapolation gives: as mean grain size is reduced to ~20 nm, Bp reaches 0.5Birr.
Average grain size: 30 nm
To do this, heat treated an internal oxidation strand with Nb-1Zr at 600C.
To find this out, we can measure Fp-B curves of a strand with even smaller grain size.
If ZrO2 particles 10 nm OD, they must be separated by 40 nm to get Nb-1% Zr

## Slide 19
Q6: Is Nb3Sn T margin too small for 16 T magnets?
Q: But we know that higher Jc makes a strand more unstable, right?
A: This sort of instability is important of lower fields where J is much higher, and the energy storage (integrated heat capacity) is less than the energy due to the FJ (Jc)
Of course, small filaments are needed for lower field FJ stability
Overall Answer: Nb3Sn high field margin is a function of B and I/Ic
Higher Jc can help achieve higher margin , with some Jc going to performance, and some to lower I/Ic and thus increased margin
If at 14 T, we are at 82% Iop, then at 16 T, Tmargin is reduced by 18%. Or, to keep Tmargin, Iop/Ic reduced 4%
IWASA
Disturbances can cause a temperature rise, T
If T > Tcs-Top, current will be shared to the matrix, and the strand will quench
Since Tc (thus Tcs)  as B , any strand has less “margin” at higher B, all else being equal
Question: Is our margin at 16 T too small?

## Slide 20: Q7: Can we realize this in a multifilamentary ternary?
We will show below our progress on multifilamentary strands
Ternaries are now being pursued, and we have several promising designs

## Slide 21
Transport layer Jc and magnetic layer Jc of the subelements
Results for a Binary subelement
So,
first we must translate this result into a multifilament
Then we must realize this in a ternary alloy strand

## Slide 22: Factors which Influence A15 grain size in the internal oxidation method
There are three key parameters which need to be optimized for a given strand (subelement) design;
(1) the level of SnO2 powder
(2) the thickness of the Nb-Zr alloy
(3) The local concentration (chemical potential) of the SnO2 (oxygen) near the Nb-Zr alloy boundary
(4) the pre-HT schedule (time for oxygen injection)
The first two are important because together they set the all-important SnO2 to Nb ratio and Nb to Sn ratio.
Too little SnO2 and no oxidation, and thus no grain refinement occurs.
Too much, and the Nb as well as the Zr will be oxidized – leading to an oxygen impervious niobium-oxide barrier at the inner wall of the tube

## Slide 23: Factors which Influence A15 grain size in internal oxidation method II
(3) The local concentration (chemical potential) of the SnO2 (oxygen) near the Nb-Zr alloy boundary
(4) the pre-HT schedule (time for oxygen injection)
The third and forth are important because they set the rate, and time for, respectively, the oxygen injection into the Nb-Zr.
In fact all of the oxygen which is injected into the Nb is done before the A15 formation reaction.
To promote oxidation (and thus grain refinement) we can use; (i) more SnO2 powder, (ii) less Nb1%Zr alloy, (iii) slower ramp rates.
Because of the differences in chemical potential depending on how the SnO2 powder is deployed (a dense layer, or distributed) these ratios and optimizations are different for different strand designs

## Slide 24: Simple Summary of Mono/Multi Strands

## Slide 25
Thick Nb barrier 61 restack- HTR
Grain size = 80 nm
Jc 12 T = 6800 A/mm2

## Slide 26
Thin Nb barrier 61 restack- HTR
Unreacted strand
Reacted strand
Grain size = 50 nm

## Slide 27
Segregated Powders B- 61 restack- HTR
Fabricated to Final size and being reacted

## Slide 28
Multi-filamentary PIT strands-Supramagnetics
S120B-625C/680h:
B, T | 11 | 12 | 12.5 | 13 | 13.25
Ic, A | > 220 | 182.8 | 157.9 | 136.0 | 123.8
n-value | - | 24.6 | 21.3 | 20.6 | 18.8
220A: limit of the power supply.
Assuming 25% of the filaments are broken: need improvement!
Transport Jc matches magnetic Jc.
The average grain size: 40 nm.
12 T Jc = 8700 A/mm2

## Slide 29
 |  | I. Present state-of-the-art RRP strands | II. The wire with SnO2 - 625 C / 800h | III. Only improve Birr to 25 T by Ti doping, etc. | IV. Only refine the grain size to 25 nm | V. Both improve the Birr to 25 T and refine the grain size down to 25 nm
Grain size, nm |  | 100 - 120 | 36 | 36 | 25 | 25
Fp-B peak |  | 0.2Birr | 0.34Birr | 0.34Birr | 0.5Birr | 0.5Birr
Fp,max, GN/m3 |  | ~90 | 180 | 180 | ~250 | ~250
Birr, T |  | 25 | 20 | 25 | 20 | 25
12 T | Layer Jc, A/mm2 | 5,000 | 9,600 | 16,400 | 20,000 | 20,800
 | Non-Cu Jc, A/mm2 | 3,000 | 5,760 | 9,840 | 12,000 | 12,480
 | Engineering Jc, A/mm2 | 1,600 | 3,050 | 5,200 | 6,360 | 6,600
 | Ic, A | 800 | 1,530 | 2,620 | 3,200 | 3,320
15 T | Layer Jc, A/mm2 | 2,700 | 3,800 | 7,800 | 12,500 | 16,000
 | Non-Cu Jc, A/mm2 | 1,600 | 2,280 | 4,680 | 7,500 | 9,600
 | Engineering Jc, A/mm2 | 850 | 1,210 | 2,480 | 4,000 | 5,100
 | Ic, A | 430 | 610 | 1,250 | 2,000 | 2,560
Engineering Jc and Ic for the five different cases:
Note: Assuming all the five cases have the same Nb3Sn area fraction with the state-of-the-art RRP strands:
the Nb3Sn area fraction in a subelement is 60%, the non-Cu area fraction in a strand is 0.53, the wire diameter is 0.8 mm.
A naive look at the limits of Jc in Nb3Sn
(Rosy scenario)

## Slide 30: But, how realistic?
We cannot forget to include the area needed for the powder (we will do that next slide)
Can we really push the Fp to 0.5? (It seems that we are well on our way)
Can we really make multis (it seems so, but more process development is required)

## Slide 31
4% area needed for oxide powder

## Slide 32: Practical Conductor Jc and Je (12 T)
Layer Jc of present day RRP, Tube and PIT is 5000 A/mm2, with 60% A15 in subelement for RRP, and 50% for PIT and Tube
At 15 T Jc is 2700 A/mm2, Jc,nonCu (RRP) = 1600 A/mm2, and Tube/PIT 1350 A/mm2
4% (volume or area)is required for the SnO2 powders
At 12 T
Using 1% Zr, with full oxidation, and moderate temperatures, layer Jc of 10 kA/mm2 seen at 12 T in mono
Assuming 50% fill factor, Jc,nonCu (12 T) should reach 4750 A/mm2
If we can implement in a RRP-like design, then Jc,nonCu (12 T) should reach 5760 A/mm2 in Binary

## Slide 33: Practical Conductor Jc and Je II (15 T)
Layer Jc of present day RRP, Tube and PIT is 5000 A/mm2, with 60% A15 in subelement for RRP, and 50% for PIT and Tube
At 15 T Jc is 2700 A/mm2, Jc,nonCu (RRP) = 1600 A/mm2, and Tube/PIT 1350 A/mm2
4% (volume or area)is required for SnO2
At 15 T
Using 1% Zr, with full oxidation, and moderate temperatures, layer Jc of 3800 A/mm2 extrapolated from 14-15 T in mono
Assuming 50% fill factor and mixed powders, tube Jc,non (15 T) should reach 1805 A/mm2 (Binary)
If we used an RRP-like design, then Jc,nonCu should reach 2165 A/mm2 15 T (Binary)
With ternary push of Bc2 to 25 T, a significant further increase would be seen at 15-18 T

## Slide 34: Comment and Simple Scaling Rules
While Internal Sn strands have greater A15 fractions, they may be more difficult to fabricate
Its likely that the best deff values for these new conductors will be seen with Tube and PIT
Thus, efforts in Tube and PIT are important, especially since ….
If we simply add grain refinement to a given Nb3Sn alloy (say, ternary) and do not shift the peak of Bc2, we can expect Jc to double at all fields
If we push the peak out the effects are greater still

## Slide 35: So, What can we expect for a ternary Tube or PIT
If we assume pinning similar to what we have already produced, with a 1% Zr alloy, and a 35-40 nm grain size
And we use standard ternary alloying to reach Birr = 25 T
Then we expect a layer Jc = 7800 A/mm2 at 15 T
At 16 T, this should reduce by 30% to 5460 A/mm2
With a 50% A15 fill factor, this gives 2750
With room for the oxide, this gives 2600 A/mm2 at 16 T as a projected possible value
This does not include
  (1) maximized Bc2/Birr from modified doping or optimized HTs
  (2) Peak shifting from 0.35-0.5
  (3) further grain refinement (2% Zr)
This gives a projected value of 2600 A/mm2, which more than meets 1500 A/mm2

## Slide 36: So…. How to add the ternary?
We choose Ti, as it leads to a better strain tolerance conductor – and, it can be added to the allow after drawing
But – you can’t add it in the same area as the SnO2 – because Ti is a powerful oxygen getter
Sn+Ti
SnO2
Nb
Pre-HT
Reaction
So, its possible to add it into the Nb-Zr to start – but we plan to add it afterward

## Slide 37: E.Barzi--Artificial Fluxon Pinning Centers for Nb3Sn (film Test bed)
The discussion so far has been about artificial pinning of grain boundaries (or perhaps enhanced nucleation), but what about standard artificial fluxon pinning centers
This topic will also be addressed in the next talk using irradiation as a limiting case. But, in the end we want a more practical second phase pinner
Staggered Electrodeposition could be a mechanism to produce such structures (additive manufacturing of pinning centers in Nb3Sn).
Below we show an inexpensive way to produce Nb3Sn thin films on Nb, and it can be used as a test bed to try different billet materials inexpensively and with fast turnaround
Our first target: The Introduction of axial ribbons to enhance transverse component of pinning
We have to come up with ribbon materials that can be cold worked, do not dissolve at 700C and do not react with Sn. Potential candidates so far are Ta, Mo and V.

## Slide 38: E.Barzi--Artificial Fluxon Pinning Centers for Nb3Sn (film Test bed)
The Nb3Sn phase is obtained by electrodeposition of Sn layers and Cu intermediate layers onto Nb substrates followed by high temperature diffusion in inert atmosphere.
Subsequent thermal treatments were realized to obtain the Nb3Sn superconductive phase.

## Slide 39: E.Barzi--Artificial Fluxon Pinning Centers for Nb3Sn (film Test bed)

## Slide 40: Summary and Conclusions
We have demonstrated grain refinement by a factor of 3 and a doubling of 12 T Jc in monofilaments
Internal oxidation can be used in many Nb3Sn strand types, including Tube (demonstrated) PIT (demonstrated), RRP/RIT (proposed) etc.
Sufficiently thick reaction layers can be formed
It is shown that Birr is not sacrificed in present best binary strands
The Fp-B curve peak can be shifted to 0.5Birr for ultra-fine grain size
Multifilamentary strands have been demonstrated with refined grains and enhanced Jc values. These need
  To be pushed to meet the even higher Jc values of their subelements
  To be optimized for area fraction and Je
  To be demonstrated for a ternary alloy with the ternary alloy Bc2
This route is very promising for future Nb3Sn development

## Slide 41: Xingchen Xu
Recent graduate of our group
PhD Thesis, OSU Materials Science Department: Prospects for Improvement in Nb3Sn conductors
Refined grain and high Jc Nb3Sn
New model for what controls stoichiometry in Nb3Sn