## Slide 1
The Introduction of substitutional and non-substitutional dopants into MgB2 in high pressure/Temperature or non-equilibrium regimes
The Ohio State University
M.D. Sumption
M.A. Susner
Y. Yang
& E.W. Collings

## Slide 2: Motivation and Outline
Substitution of C for B is well documented in MgB2
We are interested to generate site substitutions of Zr or Ti for Mg in MgB2, to change Bc2, or to generate heterostructures/secondary phases, to induce flux pinning
We have made high quality MgB2 thin films by Pulsed Laser Deposition (PLD), and have used these non-equilibrium conditions to attempt to incorporate Zr and Ti
We have also used high temperature/high pressure to melt MgB2 with Zr and Ti additions through the peritectic
Goal: To add Zr or Ti either as substitutions, or Zr- Ti-borides as fine secondary phases

## Slide 3: MgB2 thin films
to turbo
Focusing lens
KrF excimer laser,
λ=248 nm
MgB2 target mounted on rotating platform
Resistive heater (1050oC max.)
SiC (0001) substrate
Nom. 25 ns laser pulse, λ=248 nm
400 mJ max. energy (typically ~4 J/cm2 energy density) impinges upon the MgB2 target, producing significant, rapid heating of target material
A laser-induced plasma forms on the target surface
Plasma forwardly and supersoniacally ejected from interaction volume, forms “plume”
Plume impinges upon the substrate, depositing plume species on surface
SiC (0001) substrate

## Slide 4: PLD synthesis routes
PLD synthesis routes for MgB2

## Slide 5: Growth of Undoped MgB2 thin films
We have created granular MgB2 thin films with a three-step process: (1) deposition of MgB2, (2) deposition of Mg cap layer, and (3) anneal at ~700oC at 1 atm highly purified Ar
Process optimized to drive up Tc to maximum seen in PLD-synthesized MgB2 films

## Slide 6: Glancing X-ray analysis of MgB2 thin films
MgB2 thin films are deposited on SiC substrates. They are c-axis oriented and are randomly oriented in-plane

## Slide 7: TEM of Undoped MgB2
MgB2
SiC
Pt
200 nm
MgB2 thin films are ~200 nm thick with an interface layer of Mg2Si formed by reaction with the SiC substrate

## Slide 8: Addition of ZrB2 by Superstructure formation + annealing
 | ZrB2/MgB2 | Nominal %ZrB2 | Tc,onset, K (magnetic)
MgB2-164 | 0/200 | 0 | 30.4
MgB2-165 | 5/200 | 2.4 | 25.3
MgB2-166 | 10/200 | 4.8 | 22.5
MgB2-167 | 20/200 | 9.1 | 18.1
MgB2-168 | 30/200 | 13.0 | 15.0
MgB2-169 | 50/200 | 20.0 | 9.99
MgB2-172 | 70/200 | 25.9 | 5.88
Zr additions were successfully introduced, but lower Bc2
In pulses, ~ 33 pulses per MgB2 layer X 100 repeats.

## Slide 9: STEM-EDS of MgB2/ZrB2 thin films

## Slide 10: GID out of plane and in-plane diffraction
Peak shift seen in a-lattice parameter peaks

## Slide 11: Lattice parameter shifts
a-lattice parameter increases with amount of ZrB2 added
c parameter more or less constant
First clear demonstration of Zr substitution into MgB2 lattice! -- but lowers properties

## Slide 12: Heterostructures and flux pinning in high-T Superconductors
High Tc superconductors like YBa2Cu3O7 need nano-scale defects to enhance the pinning of fluxons for high J, high B applications
Anything in which the YBCO lattice is disturbed over a 0.1-1 nm scale has been suggested (e.g. precipitates, dislocations)
The most successful experiments involve the formation of heterostructures:
Layered and 3D random nano dispersions that create stress fields
Self assembled nano-columns
T.Haugan, P.N. Barnes, R. Wheeler, F. Meisenkothen, and M.D. Sumption, Nature 430, 867-870 (2004)
35 layer YBa2Cu3O7/ Y2BaCuO5 nano-dispersion array
50 nm
T.Haugan, F.Baca, M. Mullins, N.Pierce, T. Campbell, E. Brewster, P. Barnes, H. Wang, and M.D. Sumption, IEEE Trans. Appl. Supercond. 19(3), 2270-2274 (2009)
Various additives induce the formation of different heterostructure morphologies

## Slide 13: Possible Additions for MgB2 heterostructure synthesis
 | Space group | a (Å) | c (Å) | Δa, %
Ti | P63/mmc | 2.951 | 4.684 | -4.38
AlB2 | P6/mmm | 3.009 | 3.262 | -2.46
TiB2 | P6/mmm | 3.038 | 3.239 | -1.52
MgB2 | P6/mmm | 3.085 | 3.523 | --
NbB2 | P6/mmm | 3.111 | 3.266 | 0.84
UB2 | P6/mmm | 3.130 | 3.988 | 1.46
ZrB2 | P6/mmm | 3.169 | 3.531 | 2.72
Zr | P63/mmc | 3.230 | 5.145 | 4.70
CdS | P63mc | 4.142 | 6.724 | 34.3
Ag (along (111) plane) | Fm-3m | 4.142 | 6.724 | 64.86
Difficult to find materials that are chemically compatible with MgB2
Some targets are already made or purchased (Ti, TiB2, MgB2, ZrB2); others will be synthesized via high-pressure, high T apparatus
2400oC Tmax at ambient Pressure,
1700oC at 10 MPa (1500 psi)
Large amount of materials available in which to play with the effect of strain on the resulting microstructures-
Possibility of impurity dispersion
Possibility of complex heterostructure formation

## Slide 14: The high pressure furnace
High pressure vessel:
Pmax is 10 MPa (~1500 psi).
Tmax is about 2000oC
Twork is up to 1700oC

## Slide 15: The high pressure furnace

## Slide 16: SEM images for 1at% ZrB2 added bulk
ZrB2 added samples:
 | Mg | B | ZrB2 | Mg:B:ZrB2 | HT type
ZRB1% | 54.14% | 45.58% | 0.28% | 2.4:2:0.01 | HT2
ZRB5% | 33.85% | 61.54% | 4.61% | 1.1:2:0.15 | HT1
ZRB10% | 38.96% | 51.95% | 9.10% | 1.5:2:0.35 | HT2
FIBbed senction
MgB4
MgB2
Mg
MgB7?
ZrB2?

## Slide 17: TEM images for 1at% ZrB2 added bulk
FEI Helios 600 Advanced Dual-Beam SEM was used for TEM sample preparation.
~10μm in length and ~5 μ m wide slat
Bright field TEM images was obtained by Philips CM 200
<100nm

## Slide 18: Magnetic results for 10at% ZrB2 added bulk
M-T up to 6T and 50K
Double transition appeared
ZrB2: Tc=5.5K
Inhomogeneity or substitution?
22.58K
31.42K

## Slide 19: Summary
PLD thin film MgB2/ZrB2 heterostructures have been made.
Subsequently annealed, this has led to uniform Zr incorporation into the grains
The Zr is shifting the bulk lattice parameter, and also changes the Bc2 in a strong and uniform way with Zr level, suggesting Mg site substitution
STEM shows Zr uniformity within grains, Zr additions depress Bc2
High pressure induction furnace was used to push MgB2 through the peritectic, finding the correct peritectic temperature, about 1450 C.
Additions of ZrB2 led to Nano-sized particle/second phase(<100nm) widely distributed in the area close to the boundaries in 1at% ZrB2 added MgB2 ingot.
A double-transition behavior was observed in 10at% ZrB2 added sample, suggesting soe Zr introduction into the MgB2
Further work will focus on other diboride additions with various levels of lattice match, to investigate nanophase pinning structures in PLD films, and possibly site substitution as well

## Slide 20: ZrB2 and TiB2 added MgB2 ingot
Zr and Ti were collected as potential candidates for the study of homogeneity doping and Mg site substitution.
Sample preparation:
Mg turning (-4mesh,99.98%, Alfar Aesar)
B powder(-325msh,99%, Alfar Aesar)
ZrB2 powder(99.5%,,Alfar Aesar)
TiB2 powder(99.5%, Alfar Aesar)
 | a, Å | c Å | c/a | space group | Atomic weight, g/mol
MgB2 | 3.09 | 3.52 | 1.14 | P6/mmm | 45.93
ZrB2 | 3.17 | 3.52 | 1.11 | P6/mmm | 112.85
TiB2 | 3.03 | 3.23 | 1.07 | P6/mmm | 69.49
HT1:
Ramping: 500oC to 1500oC, 20oC/min
Soaking: 1500oC, 30min
Cooling: 1500oC to 500oC, 5oC/min
HT2:
Ramping: 500oC to 1700oC, 20oC/min
Soaking: 1700oC, 20min
Cooling: 1700oC to 500oC, 5oC/min
Ag Pressure: 10MPa